## Slide 1: Metals
Ch 7 and 8

## Slide 2: Types and abundances of metals
Abundant metals
  Average abundance in crust > 0.1 weight %
    Fe, Al, Mg, Mn, Si, and Ti
    Abundant enough that future availability will never be in doubt
Scarce metals
  <<0.1 weight % in crust
  Ferro-alloy metals e.g. Ni, Cr
  Base metals e.g. Cu, Pb
  Precious metals e.g. Au, Ag, Pt
  Special metals e.g. Ga, Ge, REE

## Slide 3: Iron: The backbone of industry
Iron and its alloys = 94% of all metal consumed
Abundant ores!
Ease of smelting!
Low cost!
Strong, durable, and easy to work!

## Slide 4: Iron ore minerals
OXIDES:
Hematite
Magnetite

## Slide 5
Ferrous iron = Fe2+ Reducing conditions (no oxygen present)
  More soluble
Ferric iron = Fe3+ Oxidizing conditions (oxygen present)
  Insoluble

## Slide 6: A common occurrence…
Great diversity of geologic processes which form Fe ores
  Igneous, Sedimentary, and Metamorphic

## Slide 7: Banded Iron formations (BIFs)
Most important Fe deposits today
HUGE deposits in the great lakes area of the US!
Occur only in Precambrian rocks (i.e. rocks older than 520 Ma)

## Slide 8
Alternating layers of fine grained magnetite+hematite and quartz

## Slide 9: Banded Iron formations (BIFs)
Formed on the seafloor – chemical precipitates
All formed between 2.6 and 1.8 Ga
Banding of gray (hematite and Magnetite) and red (Quartz) layers

## Slide 10: Mining enriched Fe-ores
BIF typically contain just 20-40% Iron
In some places, Intense chemical weathering has removed much of the silica/carbonate layers
  Enriched residual ores are >55% Iron
Early mining of Iron – limited to these enriched ores

## Slide 11: Great Precambrian Iron districts of the world:
Lake superior district, US
Labrador, Canada
Cerro Bolivar, Venezuela
Minas Gerais, Brazil
Hamersley, Australia
Krivoi Rog, Russia

## Slide 12: In Lake Superior District
These enriched portions of BIF ores were nearly all mined out by early 1900’s
How can we concentrate lower grade BIFs?
  Grind the rock to powder
  Separate Fe oxides from silicates
  Mix with clay and form into pellets (~65% Fe)

## Slide 13: Blast furnaces smelting
Coke
Notes: Origins ~1340 AD, evolved to present form
Cylindrical shaft lined with refractory material – bricks hard to melt
Coke is a fuel with few impurities and a high carbon content, usually made from coal. It is the solid carbonaceous material derived from destructive distillation of low-ash, low-sulphur bituminous coal. Cokes made from coal are grey, hard, and porous. The carbon monoxide produced by its combustion reduces iron oxide (hematite) in the production of the iron product.
1 Metric ton Iron = 1.6 mt of pellets + 0.7 mt of coke + 0.2 mt of limestone + 3.6 mt of hot air (1600°C/3000°F)
Chemical reactions  coke combusts to form CO
CO reduces Fe-oxides to Fe metal (and itself is oxidized to CO2)

## Slide 14: History of American steel industry
During IR, American settlers mined small iron deposits in the Appalachians
In 1845 – the Lake Superior BIFs were discovered
Iron production shifted from Europe to the US – US dominated world Fe production from ~1900-1970
  BIFs
  Coal
  Limestone

## Slide 15: History of American steel industry
Production declined in Europe (and Japan) due to WWI, Great Depression, and WWII
  US industry remained intact! Lion’s share of the world market ~1950s (47%)
But then… Europe and Japan rebuilt… with upgrades
  Japan and China had cheap ocean shipping access to HUGE and very low-cost Fe deposits in Australia
  Newer plants, lower operating costs
In 2008, US had just 7% of world Fe market
  ~50% of steel mills and furnaces have shut down since the 70’s
  ~60% decrease in jobs in this industry (20,000 to 7,500)
Notes: Newer plants, lower operating costs
~50% of steel mills and furnaces have shut down since the 70’s
~60% decrease in jobs in this industry (20,000 to 7,500)

## Slide 16: Aluminum
2nd most abundant metal (after Si)
BUT very difficult to free from most mineral forms
  Only been mined for last 125 years
2nd most widely used metal (after Iron)

## Slide 17: Aluminum use today
US uses the most aluminum (44 lbs/person/yr)
  Transportation (38%)
  Packaging (22%)
  Building materials (16%)
  Electrical (7%)
  Other consumer goods (7%)
~150 lbs/car
High strength to weight ratio
>100 billion cans made in US each year

## Slide 18: Al ore: Bauxite (material composed of Al hydroxides)
Formed in Laterite soils!
Subtropical to tropical climates
Abundant rainfall
Aluminous parent rocks (feldspars)
Sweet spot of topographic relief
  High enough that there is drainage
  Low enough that mechanical erosion of soil is slow relative to chemical leaching

## Slide 19: Chemical weathering in lateritic conditions
Least soluble components:
  SiO2
  Al2O3
  Fe2O3
More soluble Na+, K+, Mg+, and Ca2+ is removed in solution
Decaying organic matter makes groundwater slightly acidic – dissolves much of the clays, silica and Fe minerals
Leaves Al-hydroxides (and some Fe-hydroxides) behind

## Slide 20: Aluminum production
Easy to mine the ore (soft, forms at the surface)
Processing that ore is VERY energy intensive
Bauxite mines are generally in tropical regions
 often in countries where energy is not cheap
 far from biggest markets of aluminum products
So the Bauxite ore is washed, dried and shipped to other countries like Norway, Canada, and the US

## Slide 21
Notes: mined, crushed, washed, dried and shipped
Make ore into alumina (Al2O3)
Then put alumina into molten cryolite (Na3AlF6) bath – this is both an electrolyte and solvent – reduces alumina to aluminum metal
This is high energy because temperature has to be maintained at 950°C, voltages must remain at 1000 volts, and electric currents at 150,000 amperes

## Slide 22
Notes: Most Al smelting powered by hydrothermal plants. One coal fired plant in Aus, and they are building a geothermal energy plant in Iceland

## Slide 23: History of Al industry in US
Growth coincided with development of major power networks and building of major hydroelectric facilities
Leveled off after 1973 oil embargo when energy costs rose

## Slide 25: Energy use
Much higher energy than other common metals
MUCH less energy needed to recycle aluminum, than for primary production
Notes: And this is for bauxite – the easiest Al bearing material to smelt
Importance of recycling – energy saving by 95%

## Slide 26
Gasoline
Japan example
Notes: Japan – 1985 – closed primary Al production
100% Import Al scrap metal – this is awesome – its essentially like importing energy – as other countries put in the energy to produce that aluminum initially

## Slide 27: Titanium
Only been used on large scale for 50 yrs
Alloys – high strength to weight ratio, melting point, and corrosion resistance
White titanium oxide pigment
  White, opaque, permanence of color, low toxicity
  Principal pigment in paint, paper, plastic, rubbers and more
Notes: Before that – white Pb oxide was used

## Slide 28: Ti Ores
Mafic minerals like Magnetite and ilmenite (layered mafic intrusions)
Heavy Ti bearing minerals (illmenite and rutile) are also formed in small quantities in many igneous and metamorphic rocks, which when reduced to a sediment, can be separated by density (placer deposits)

## Slide 29: Processing of Ti
Mining is pretty low impact (especially beach placer deposits)
However processing produces a large amount of toxic sulfate and sulfuric acid waste
  Used to be dumped into streams and oceans  Now we deal with it in acid neutralization plants
  We are still dealing with run off from old plants…

## Slide 30: Mg
USES:
Alloys, cement, rubber
ORES:
Seawater!
Dolomite
Notes: Draw illustration on Pg 260

## Slide 31: Si
USES:
Photovoltaic cells
Resins, lubricants, rubbers, and much more
ORES:
Molten quartz
  VERY high energy

## Slide 32: Manganese
USES:
steel production
  Scavenges impurities from steel!
ORES:
Chemical precipitates (hydrothermal vents – VMS deposits)
Notes: Also used in water purification (K permanganate) and dry cell betteries